How to Make a Ferrofluid

Preparation of the Ferrofluid

- Add 4 mL of the FeCl3 solution (0.004 mol) and 1 mL of the FeCl2 solution (0.002 mol) to a 150 mL beaker.

- While swirling the iron chloride solution, slowly add 50 mL of 0.5 M ammonium hydroxide dropwise over 5 minutes.  Picture A

- A black precipitate should form during the slow addition.  This is magnetite.  Picture B

- After all the ammonium hydroxide has been added, stop swirling.

- Place one of the bar magnets under the beaker.  It should pull all of the magnetite out of the solution, and the water should become clear.  Picture C

- Keeping the magnet on the bottom of the beaker, pour off the excess water.

- Add a minimal amount of water and transfer the magnetite to a weigh boat.

- Place the magnet under the weigh boat to settle the magnetite.

- Pour off the excess water.

- Rinse the magnetite two more times by adding a small amount of water, using the magnet to settle the magnetite, and discarding the clear water.

- Remove as much water as necessary to form a viscous fluid.  Be careful NOT to remove all of the water, or you will form a solid.

- Add 1 mL of the 25% tetramethylammonium hydroxide solution, and mix the ferrofluid for 2 minutes by moving the weigh boat over the magnet.

- Once thoroughly mixed, place the magnet under the weigh boat and remove the excess black liquid into an empty beaker, as you did before during the rinsing.

- Place the magnet under the ferrofluid and move it until you see spiking.  Picture D

Did you make a successful ferrofluid?

Discussion Questions

- What is the molarity of the FeCl3 and FeCl2 solutions?

- Why do you think slow (dropwise) addition of ammonium hydroxide is important?  What might happen if you add the ammonium hydroxide quickly?

- Magnetite, Fe3O4, consists of iron in what oxidation states?

- Why do you place a magnet underneath the beaker while removing the water?

- What is the purpose of the stabilizing agent tetramethylammonium hydroxide?  What might happen if NO stabilizing agent is used?

- Describe what happens when a magnet is brought near a ferrofluid.  What happens when the magnet is removed from the ferrofluid?

- ADVANCED:  Balance the following equation.

__ FeCl3 + __ FeCl2 + __ NH3 + __ H2O → __ Fe3O4 + __ NH4Cl

Copyright © 2003 by Sarah Tolbert. All rights reserved; revised 2007

# Text boxes

D

A

C

B